 TECHNICAL DATA SHEET                                                                                                           


U/UTP 4Pairs cable-category5E-LSZH Sheath
	Content of the Data Sheet

	Sheath Printing
	TBD

	Customer No.
	
	Customer Reference
	
	[image: image1][image: image2.wmf]

	Category
	U/UTP CAT5E-4P- LSZH(IEC60332-1)
	

	Reference Standard
	ISO/IEC11801、TIA-568-C.2
	

	Conductor
	Material
	Solid-Bare Copper
	

	
	Nom.O.D.(mm)
	0.495
	up
	+0.005
	

	
	
	
	down
	-0.005
	

	Insulation
	Material
	HDPE
	

	
	Diameter
	0.87±0.05mm 
	

	Sheath
	Thickness
	0.50±0.05 mm 
	Technical Performance(100m):

Frequency RL         ATT         NEXT  　 Phase  DELAY

(MHz)     ≥dB 　    ≤dB     　 ≥dB        ≤ns

1        20.0       2.0         65.3        570.00

4.0       23.0       4.1         56.3        552.00

8.0       24.5       5.8         51.8        546.73

10.0      25.0       6.5         50.3        545.38

16.0      25.0       8.2         47.2        543.00

20.0      25.0       9.3         45.8        542.05

25.0      24.3       10.4        44.3        541.20

31.25     23.6       11.7        42.9        540.44

62.5      21.5       17.0        38.4        538.55

100       20.1       22.0        35.3        537.60

Frequency PSNEXT           ELFEXT          PSELFEXT

(MHz)      ≥dB             ≥dB             ≥dB

1          62.3             63.8              60.8

4          53.3             51.8              48.8

8          48.8             45.7              42.7 

10         47.3             43.8              40.8

16         44.4             39.7              36.7

20         42.8             37.8              34.8

25         41.3             35.8              32.8

31.25      39.9             33.9              30.9

62.5       35.4             27.9              24.9

100        32.3             23.8              20.8



	
	External O.D.
	5.0±0.4 mm 
	

	
	Surface
	Clean,Frap,Satiation
	

	
	Material
	LSZH(complies RoHS)，IEC60332-1
	

	
	Color
	TBD
	

	Surface Printing
	Letter height
	3.0±0.3mm
	

	
	Color
	Black
	

	
	Print error & Space
	≤±0.5%，1m
	

	Core Color
	1 White- Blue /Blue
	2 White-Orange /Orange
	

	
	3 White- Green /Green
	4 White- Brown /Brown
	

	Packing
	Wooden Tray & Carton
	

	Carton

dimension
	According to the requires
	

	Packing length
	(305±1.5)m
	

	Rip-cord
	Yes
	Drain wire
	No
	

	Sheath Physical

Properties
	Before Aging  Tensile Strength (Mpa)  ≥10.0
               Elongation(%)        ≥125
	

	
	Aging Period(℃×hrs)     100℃×24h×7d
	

	
	After Aging  Tensile Strength(Mpa)     ≥8.0
           Elongation(%)             ≥100
	

	
	Cold bend(-20±2℃×4h)  8×Cable O.D.，No visible cracks
	

	Electrical

Characteristics

 (20℃)
	1.0-100.0MHz  Impedance(Ω)              100±15
	

	
	1.0-100.0MHz  Delay Skew (ns/100m)         ≤45
	

	
	DC ResistanceΩ/100m) max                    9.5
	

	
	DC Conductor Resistance Unbalance(%) max        5.0
	

	Version
	A/01
	Date
	2017-08-25
	Revised By
	Caihanglie
	Audited By
	Nidonghua
	Approved By
	Nidonghua


White- Brown /Brown





White-Orange/Orange





White-Blue /Blue





White- Green /Green





Rip-cord





Sheath





� EMBED  \* MERGEFORMAT ���










_1234567890.unknown

